APPENDIX C

WEIGHTS OF BUILDING MATERIAL

Material						Weight, lb/sq. ft

Ceilings

Plasterboard,  non-plastered					3

Plaster, 3/4 in, and wood lath					8

Plaster on tile or concrete						5

Suspended, metal lath and plaster					10

Floors

Hardwood flooring, 7/8 in. thick					4

Sheathing, yellow pine 1 in. thick					4

Spruce								2-1/2

Wood block, creosoted  3 in. thick					15

Cement finish per in. thick					12

Terrazzo tile per in. thick including base				12

Gypsum Slab, per in thick						5

Roofs

Corrugated metal, galvanised:

20 gauge						1.66

24 gauge						1.16

28 gauge						0.78

Roofing felt, 3 ply and gravel					5-1/2

Roofing felt, 5 ply and gravel					6-1/2

3 ply ready roofing						1

Shingles, wood							3

Tile or slate							5 to 20

Partitions

Channel Studs, metal lath, cement plaster,

solid 2 in. thick						17.5

Studs, 2" x 4", wood or metal lath,

3/4 in. plaster both sides					18

APPENDIX C (Cont'd)

Studs, 2" x 4", plaster board,

1/2" plaster both sides					18

Plaster, 1/2" on clay tile (one side)					4

Mortar Rubble Masonry

Limestone							150

Dry Rubble Masonry

Limestone							125

Earth etc Excavated

Sand, gravel, dry, loose						90 to 105

Sand, gravel, dry, packed						100 to 120

Clay, dry							63

Clay, damp, plastic						110

Clay, and gravel, dry						100

Earth, dry, loose							 76

Earth, dry, packed						 95

Earth, moist, packed						 96

Earth, mud packed						115

Rip-rap, limestone						80 to 115

Excavations in Water

Sand or gravel							60

Sand or gravel and clay						65

Clay								80

River mud							90

Soil								70

Stone rip-rap							65

Concrete Block

8" x 8" x 16" (from the US)					35 to 40 lbs. per block

8" x 8" x 16" (from the Dominican Republic or

other areas with igneous or

extrusive rock)					45 to 50 lbs per block

APPENDIX C (Cont'd)

Concrete

With aggregate (basalt or other extrusive rocks)

eg. from Haiti, Dominican Republic				155 to 160 lbs./cu. ft

With aggregate (sedimentary rock),

from Jamaica, Bahamas and

other quarries							145 to 150 lbs./cu. ft

With aggregate from limestone (local sources)				140 to 145 lbs./cu. ft