APPENDIX E

WEIGHTS OF BUILDING MATERIAL

Material								Weight, lb/sq.ft

Ceilings

Plasterboard, unplastered						3

Plaster, 3/4 in, and wood lath						8

Plaster on tile or concrete						5

Suspended, metal lath and plaster					10

Floors

Hardwood flooring, 7/8 in thick						4

Sheathing, yellow pine 1 in. thick						4

Spruce									2-1/2

Wood block, creosoted 3 in thick					15

Cement finish per in. thick						12

Terrazzo tile per in. thick including base					12

Gypsum Slab, per in thick						5

Roofs

Corrugated metal, galvanised:

20 gauge							1.66

24 gauge							1.16

28 gauge							0.78

Roofing felt, 3 ply and gravel						5-1/2

Roofing felt, 5 ply and gravel						6-1/2

3 ply ready roofing							1

Shingles, wood								3

Tile or slate								5 to 20

Partitions

Channel Studs, metal lath, cement plaster,

solid 2" thick							17.5

Studs, 2" x 4", wood or metal lath,

3/4 in. plaster both sides					18

APPENDIX E (Cont'd))

Studs, 2" x 4", plaster board,

1/2" plaster both sides						18

Plaster, 1/2" on clay tile (one side)					4

Mortar Rubble Masonry

Limestone								150

Dry Rubble Masonry

Limestone								125

Earth etc Excavated

Sand, gravel, dry, loose							90 to 105

Sand, gravel, dry, packed						100 to 120

Clay, dry								63

Clay, damp, plastic							110

Clay, and gravel, dry							100

Earth, dry, loose							76

Earth, dry, packed							95

Earth, moist, packed							96

Earth, mud packed							115

Riprap, limestone							80 to 115

Excavations in Water

Sand or gravel								60

Sand or gravel and clay							65

Clay									80

River mud								90

Soil									70

Stone riprap								65

Concrete Block

8" x 8" x 16" (from the US)						35 to 40 lbs per block

8" x 8" x 16" (from the Dominican Republic or

other areas with igneous or

extrusive rock)						45 to 50 lbs per block

APPENDIX E (Cont'd)

Concrete

With aggregate (basalt or other extrusive rocks)

eg from Haiti, Dominican Republic				155 to 160 lbs/cu.ft

With aggregate (sedimentary rock),

from Jamaica, Bahamas and

other quarries							145 to 150 lbs/cu.ft

With aggregate from limestone (local sources)				140 to 145 lbs/cu.ft